# Growth rate vs temperature for DEZ/ H2O, TiCl4/ H2O og TMA/H2O

## DEZ/ H2O

Atomic layer epitaxy growth of doped zinc oxide thin films from organometals (Vesa Lujala *, Jarmo Skarp, Markku Tammenmaa, Tuomo Suntola)

Reactor: F-120

Substrate: Soda lime glass (50 X 50 mm)

Puls/purge: 0,2 s DEZ  - purge 0,4 – 0,2 s H2O – 0,4 purge

## A1303 thin film growth on Si (100) using binary reaction sequence chemistry

A.W. Ott, J.W. Klaus, J.M. Johnson, S.M. George

Reactor: ?

Substrate: Si(100)

Puls/purge: 0,5s TMA  -  20 s purge - 0,5s H2O  -  20 s purge

## TiCl4/ H2O

! The growth rate vs temperature for TiO2 has been reported differently in articles, without anyone trying to describe why it is so different…

Growth of titanium dioxide thin films by atomic layer epitaxy (Mikko Ritala and Markku Leskel/i, Erja Nykfinen, Pekka Soininen and Lauri Niinist6)

Reactor: F-120

Substrate: Soda lime (square)

Puls/purge: 0,2 s TiCI4  - purge 0,5 – 0,2 s H2O – 0,5 purge

Morphology and structure of TiO 2 thin films grown by atomic layer deposition (Jaan Aarik a, Aleks Aidla a Teet Uustare a,*, V~iino Sammelselg)

Reactor: JSM-35 (?)

Substrate:QCM

Puls/purge: ?